Low-cost and scalable manufacturing of optical metasurfaces in the visible using engineered optical materials

(PER, low-loss a-Si:H, and hybrid ALD structural resin)

Junsuk Rho*1,2,3,4

1Department of Mechanical Engineering, Pohang University of Science and Technology (POSTECH), Pohang, Republic of Korea 37673

2Department of Chemical Engineering, Pohang University of Science and Technology (POSTECH), Pohang, Republic of Korea 37673

3POSCO-POSTECH-RIST Convergence Research Center for Flat Optics and Metaphotonics, Pohang, Republic of Korea 37673

4National Institute of Nanomaterials Technology (NINT), Pohang, Republic of Korea 37673

E-mail: jsrho@postech.ac.kr

Here, we demonstrate low-cost, scalable manufacturing of optical metasurfaces with three approaches: 1) increasing a refractive index of resin with dielectric particle embedding for single-step nanoimprinting[1-5], 2) suppressing optical losses of hydrogenated amorphous silicon (a-Si:H) to apply complementary-metal-oxide-semiconductor technologies[6], and 3) high-index atomic layer deposited (ALD) structural resin[7]. We demonstrate the effectiveness of these materials in creating optical metasurfaces operating at different wavelengths in the infrared, visible, and ultraviolet spectra. Firstly, we achieve high efficiencies of up to 90.6%, 47%, and 60% with a-Si[1], TiO2[2-4], and ZrO2 PER[5] at wavelengths of 940, 532, and 325 nm, respectively. Furthermore, we obtain a measured efficiency of 30% at a wavelength of 248 nm using ZrO2 PER metasurfaces[5]. Secondly, by adjusting the deposition conditions of plasma-enhanced chemical vapor deposition, we engineer the bandgap of a-Si:H to enable low-loss operation, with minimum extinction coefficients as low as 0.082 at 450 nm[6]. Using low-loss a-Si:H, we demonstrate efficient beam-steering metasurfaces with measured efficiencies of 42%, 65%, and 75% at 450, 532, and 635 nm, respectively, marking the first Si-typed metasurfaces working at the full visible. Finally, we manufacture highly efficient metalenses using hybrid ALD structural resin with deep-ultraviolet lithography at visible wavelengths. Their measured efficiencies approach 60.9%, 77.8%, and 64.8% at 450, 532 and 635 nm, making them suitable for ultrathin virtual reality devices. Our approach using PER[1-5], low-loss a-Si:H[6], and hybrid ALD structural resin[7] enables the low-cost, large-area manufacturing of efficient optical metasurfaces across different wavelengths, facilitating the commercialization of metasurface-based photonic devices[8-13].

Reference:

- Yoon, G.; Kim, K.; Kim, S.-U.; Han, S.; Lee, H.; Rho, J.; “Printable Nanocomposite Metalens for High-Contrast Near-Infrared Imaging” ACS Nano 2021 15(1) 698-706.

- Kim, K.; Yoon, G.; Baek, S.; Rho, J.; Lee, H.; “Facile Nanocasting of Dielectric Metasurfaces with Sub-100 nm Resolution” ACS Appl. Mater. Interfaces 11(29) 26109-26115.

- Yoon, G.; Kim, K.; Huh, D.; Lee, H.; Rho, J.; “Single-step Manufacturing of Hierarchical Dielectric Metalens in the Visible” Nat. Commun. 2020 11 2268.

- Kim, J.; Oh, D. K.; Kim, H.; Yoon, G.; Jung, C.; Kim, J.; Badloe, T.; Kang H.; Kim, S.; Yang, Y.; Lee, J.; Ko, B.; Ok, J.G.; Rho, J.; “Metasurface Holography Reaching the Highest Efficiency Limit in the Visible via One-step Nanoparticle-Embedded-Resin Printing” Laser Photonics Rev. 2022 16(8) 2200098.

- Kim, J.; Kim, W.; Oh, D.K.; Kang, H.; Kim, H.; Badloe, T.; Kim, S.; Park, C.; Choi, H.; Lee, H.; Rho, J.; “One-step Printable platform for High-Efficiency Metasurfaces Down to the Deep-Ultraviolet Region” Light Sci. Appl. 2023 12 68.

- Yang, Y.; Yoon, G.; Park, S.; Namgung, S.D.; Badloe, T.; Nam, K.T.; Rho, J.; “Revealing Structural Disorder in Hydrogenated Amorphous Silicon for a Low-loss Photonic Platform at Visible Frequencies” Adv. Mater. 2021 33(9) 2005893.

- Kim, J.; Seong, J.; Kim, W.; Lee, G.-Y.; Kim, S.; Kim, H.; Moon, S.-W.; Oh, D.K.; Yang, Y.; Park, J.; Jang, J.; Kim, Y.; Jeong, M.; Park, C.; Choi, H.; Jeon, G.; Lee, K.-I.; Park, N.; Lee, B.; Lee, H.; Rho, J.; “Scalable Manufacturing of High-Index Atomic Layer-Polymer Hybrid Metaphotonics in the Visible” Nat. Mater. 2023 22 474-481.

- Kim, G.; Kim, Y.; Yun J.; Moon, S.-W.; Kim, S.; Kim, J.; Park, J.; Badloe, T.; Kim, I.; Rho, J.; “Metasurface-Driven Full-Space Structured Light for Three-Dimensional Imaging” Nat. Commun. 2022 13 5920.

- Kim, I.; Kim, W.-S.; Ansari, M.A.; Mehmood, M.Q.; Badloe T.; Kim, Y.; Gwak, J.; Lee, H.; Kim, Y.K.; Rho, J.; “Holographic Metasurface Gas Sensors for Instantaneous Visual Alarms” Sci. Adv. 2021 7(15) eabe9943.

- Kim, I.; Ansari, M.A.; Mehmood, M.Q.; Kim, W.-S.; Jang, J.; Zubair, M.; Kim, Y.-K.; Rho, J.; “Stimuli-Responsive Dynamic Metaholographic Display with Designer Liquid Crystal Modulators”Adv. Mater. 2020 32(5) 2004664.

- Jung, C.; Kim, G.; Jeong, M.; Jang, J.; Dong, Z.; Badloe, T.; Yang, J.K.W.; Rho, J.; “Metasurface-Driven Optically Variable Devcies” Chem. Rev. 2021 121(21) 13013-13050.

- Kim, I.; Martins, R.J.; Jang, J.; Badloe, T.; Khadir, S.; Jung, H.-Y.; Kim, H.; Kim, J.; Genevet, P.; Rho, J.; Nat. Nanotechology 2021 16 508-524.

- Rho, J; “Metasurfaces: Subwavelength Nanostructure Arrays for Ultrathin Flat Optics and Photonics” MRS Bulletin 2020 45 180-187.